## Slide 1
Objectives:
Investigate Berry-curvature related effects in photocurrent response of topological semimetals
Compare nano-infrared/nano-photocurrent
Published and submitted results:
Yinming Shao et al (Nature Physic (in press))
Yinming Shao et al (in preparation)
Results 3: “hot-spots” for thin flakes (~ 12 nm)
Nano-infrared Studies of Topological Semimetals
Yinming Shao, Columbia University, Collaborators: Sanghoon Chae (Columbia),
Eve Emmanouilidou (UCLA), Ni Ni (UCLA), James Hone (Columbia), Dimitri Basov (Columbia)
Energy Frontier Research Center funded by the U.S. Department of Energy, Office of Science, Basic Energy Sciences (BES), under award DE-SC0019443
Background:
Results 1:
Results 2:
Summary and future plans :
TaIrTe4 is an inversion-symmetry-breaking type-II Weyl semimetal [1] that has recently been shown to exhibit giant photocurrent response in mid-infrared wavelength range [2].
Crystal structure (left panel) and the corresponding Weyl points in momentum space (right), from Ref. [1].
Optical (left) and photocurrent (right) image of TaIrTe4, scale bar 20 um, from Ref. [2]
Previous diffraction-limited photocurrent imaging study [2] has established very strong current response around 4.5 um and it has been claimed to result from Berry curvature enhancement. We use state-of-the-art nano-optical/photocurrent imaging techniques to further investigate the Berry curvature related effects.
[1] I. Belopolski et al, Nat. Commun. 8, 942 (2017)
[2] J. Ma et al, Nat. Mater. 18, 476 (2019)
Near-field (O3)
Photocurrent (A3)
Sample: TaIrTe4
Reference: Au contact
Optical image of a ~100 nm TaIrTe4
thin flake on SiO2/Si substrate
By shining light on a metallic AFM tip,
we get localized optical response
function/photocurrent with ~30 nm spatial resolution at infrared wave-length (1~100 um).
Comparison of Nano-infrared and
Nano-photocurrent at 4.5 um
for thick TaIrTe4 flakes
Power and frequency dependence
The near-field photocurrent shows linear power law behavior at low power, consistent with 2nd order response. At higher power the power dependence deviates from linear, while the (Au normalized) near-field optical signal remains flat with different incident laser power.
Power dependence at 4.5 um/7.3 um on thick flake
Frequency dependence
Nano-photocurrent at 1600 for a ~12 nm thin flake shows very localized (< 300 nm)
“hot-spots” for strong photocurrent, not evident in previous studies on thicker flakes.
Moreover, the photocurrent signal exhibits interesting “sign-changing” behavior multiple
times near the Au contacts. The sign reversal is present and more complicated in thick
flakes. Theoretical understanding for this behavior is currently lacking.
An increase of photocurrent as the light frequency approaches 1600 while the (un-normalized) near-field optical signal follows a gradual increase as frequency lowers.
1. More frequency dependent nano-photocurrent for
TaIrTe4 and related topological semimetals.
2. Perform low-temperature nano-photocurrent studies
to better understand the origin of the ‘sign-changing’
behavior of the nano-photocurrent map
3. Explore nano-photocurrent response in monolayers
of topological semimetals.